## Slide 1: TUNGSTEN FOAM ARMOR DESIGN
S. Sharafat, M. Andersen, Q. Hu, and
N. Ghoniem
University of California Los Angeles
High Average Power Laser Program Workshop
University of Wisconsin
Madison, WI
Sept. 24-25, 2003

## Slide 2: Outline
Design Approach:
  Loading Conditions
Thermal Design
  Transient
  Steady State
Helium Management
  Effective Medium:
    Single Pulse & Steady State
  Space-Time Diffusion in Ligaments
  He-Recycling Coefficient of W-Foam

## Slide 3: W-Foam Design Approach
He in
He out
He in
Solid
Foam
APPROACH:
Optimize W-Foam Features for:
  High “Thermal Shock Absorption:”
    Quasi-Volumetric Energy Deposition
    Flexible Structure
  “Helium Breathable” Structures:
    Large and Open Internal Surface Area
    Ligament Sized for Maximum He-Release
  Armor-Structure Interface Reliability:
    Minimize Interface Temperature Rise
    Minimize Interface Stress Mismatch
GOAL: Develop Micro-Engineered FW-Armor and Corresponding Analysis Tools for Mitigation of Severe X-rays and Fast Ion Effects on Structures.
X-rays & Ions
Solid
Foam

## Slide 4: Material Design Task
Design Parameters:
  Ligament Size
  Cell size (ppi)
Effects on Thermal Design:
  Steady State:
    Increasing PPI reduces conductivity
  Transient:
    Reducing Ligament size increases Tmax
Helium Management:
  Reduction in Ligament size increases Helium release

## Slide 5: W-Foam Material Design Parameters
Parameter | Impact | Current | Target
Pores per inch (ppi) | Heat Conduction | 40 – 100 ppi | 200 – 1000 ?
Ligament size | Small size needed for helium management | 20 – 40 um | < 5 um ?
Unit Cell Structure | Stress States | dodecahedra, tetrakaide-cahedra. | ?
Cell Anisotropy | Stress, Thermal diffusivity | Mostly Isotropic | Anisotropic
Ligament Core Material | Forms Carbides (WC&W2C) Max Temp. | Carbon | HfC, ZrC, NbC,TaC

## Slide 6: W-Foam He/Damage Conditions
Pulsed Damage and He-Implantation Rates are Enormous:

## Slide 7
Thermal Design:
  Transient
  Steady State

## Slide 8: Solid Modeling & FEM Mesh
Cell structure modeled after truncated octahedron.
Stacked into a 64 cell matrix.
Placed upon steel wall so that only tungsten is viewable.
Upper surfaces mapped out for later load conditions.
ANSYS used to find results.

## Slide 9: Transient Temperature Response
0.2 second pulse consisting of x-rays, neutrons and ions.
Surface temperature profile over heat pulse.

## Slide 10: Transient Temperature Distribution
Unlike real W-foam ligaments, our model has sharp edges.
Maximum temperatures along edges are overestimated.
Model demonstrates quasi-volumetric heating.

## Slide 11: Individual Ligament Time Heating

## Slide 12: Individual Ligament Time Heating
Top Surface
2nd Level
3rd Level
Bottom Surface

## Slide 13: Interface Behavior
Does the Tungsten-Steel interface withstand the pulse?
Does the W-foam act too much like an insulator?
Solid tungsten layer for extra protection.

## Slide 14: Steady State Analysis
Loading:
  41 MJ / shot 0.39 MW/m2 average surface heat load for a 6.5 m chamber
  hcoef = 10,000 W/m2-K
  Tcool= 400oC
Tungsten:
  (1) kligament = k (W)
  (2) kligament = 0.5 k (W)
Steady state:
  (1) Tmax ~ 600oC
  (2) Tmax ~ 642oC

## Slide 15
HELIUM MANAGEMENT
  Effective Medium:
    Single Pulse & Steady State

## Slide 16: Helium Management
About ~1020 He/shot
For 6.5 m chamber equivalent: ~ 10% of W in 5.5 hr ~ 44% of W in 1 day
Helium arrives with Ion-induced Damage:  Helium Gets trapped.
How much of the He/shot remains trapped?
Determine Primary helium trapping processes:
  Small Clusters (HeV, He2V, …)
  In Bubbles
  At Dislocations
  At Precipitates
  At Grain Boundaries
  or …
Based on primary helium trapping knowledge drive He out:
  Utilizing T-transient
  Foam features
Develop Full Scale Rate Theory for effective medium:
  Damage zone (~5 um)
  Transients of Temp., Damage, He
Use 1-D Space-Time Model for “Effective” Helium Diffusion.:
  Through Foam Ligament (10 to 30 um)
Problem:
Strategy:
Solution:

## Slide 17: Full Scale Rate Theory
A model consisting of 18 Rate Equations plus appropriate Rate Constants was developed for:
  (1) Vacancies, (2) Interstitials,
  (3) Di-Interstitials, (4) He,
  (5) HeV, (6) He2V,
  (7) He2, (8) Vac.-Clusters,
  (9) Int.-Clusters, (10) Bubble-Nucleus,
  (11) Bubbles, (12) Interstitial Loops,
  (13) Grain Boundaries, (14) Precipitates, …
SRIM calculations were used to determine damage rates, deposition profiles, and energies for Helium and Hydrogen.
10-30 um
Grain Boundary

## Slide 18: Steady-State:
Implantation
T=650oC
Disl. Density = 109/cm2 Grain size = 30 um
Precipitates = 109/cm3 Gdpa = 2.15e-3 dpa/s
GHE = 5.85e-6 He/at-s
Gradual and steady increase in Bubble Conc.
Bubbles
Vac.
Int.
1-He
He @ GB
He in BB

## Slide 19: Pulsed He/Damage at Constant Temperature:
Implantation
Bubble concentration levels off
Vac.
Int.
1-He
T=650oC
HeV

## Slide 20: Pulsed He/Damage with Temperature Spike:
Helium at GB  Helium Released
Implantation
Grain Size ~ Ligament Radius~ 10 um
650oC
650oC
1.E-23
1.E-18
1.E-13
1.E-08
1.E-03
1.E+02
1.E+07
1.E+12
1.E+17
1.E-15
1.E-13
1.E-11
1.E-09
1.E-07
1.E-05
1.E-03
1.E-01
1.E+01
TIME (s)
NUMBER / cm3
C-vac
C-int
C-He
CHeV
C-Bubble
He_in_PPT
He_in_GB
“Trapped”
Helium
T-Spike
HeV
Bubbles

## Slide 21: Pulsed He/Damage with Temperature Spike:
Implantation
1500oC
At 1500oC almost no Bubbles Survive
T-Spike
“Trapped”
Helium
HeV
Bubbles
Grain Size ~ Ligament Radius~ 10 um

## Slide 22: Helium Trapped/Released Distribution
He in small Cluster:
He, HeV, He2V, B-Nucl
99% He at Grain Boundaries
~He Released from Ligaments:
He in Bubbles
He at PPT
T = 650oC
~1%Trapped Helium
T = 650oC
Grain = 30um
Ligament Size~30 um

## Slide 23: Helium Trapped/Released Distribution
<0.1% Trapped Helium
T= 1500 C
T = 1500oC
Grain = 30um
Ligament Size~30 um

## Slide 24
0m
20m
Evac1.5
EHe0.2
5m
Emeff
x
Spatial Diffusion Model for Helium Release

## Slide 25
Slab = 20m
Slab = 10m

## Slide 26: Summary and Future Activities
Conclusions:
Thermal transient analysis shows W-foam to be a viable armor material.
Armor-structure interface mismatch issues are minimized using W-foam.
W-foam’s open cell structure plus small ligament size of order of Grain Boundaries significantly enhances helium release during early stages of He-implantation.
Ongoing Activities:
Analyze thermal stress transients.
Perform a more-detailed 1-D space-time diffusion analysis for helium release through ligaments.
Address the large Hydrogen-implantation effects.
Address foam-metal bonding issues.
Optimize foam structures.

## Slide 27: Additional Slides

## Slide 28: W-Foam Thermal Loading Conditions
1.76x1016 W/m3

## Slide 29: Key Defect Parameters

## Slide 30: References for Defect Parameters
Worthing, A.G., Phys. Rev. [2] 10 [1917] 3288/9.
Kraftmakher, Ya. A., Strelkov, P.G., Soviet Phys.-Solid State 8 [1966] 838/41.
Johnson, R.A.; Phys. Rev. [3] B27 [1983] 2014/8.
Vingsbo, O. Mater. Sci. Eng. 8 [1971] 32/40.
Vandervoort, R.R., Trans. AIME 242 [1968] 345/7; 245 [1969]2269/72.
Maury, F., Biget, M., Vajd, P., Lucasson, A., P., Radiation Eff. 38 [1978]53/65.
Scanlan, R.M., Styris, D.L., Siedman, D.N., Phil. Mag. [8] 23 [1971] 1439/57, 1459/78.
Seidman, D.N., Wilson, K.L., Nielsen, C.H., Phys. Rev. Letters 35 [1975] 1041/42.
Schultz, H., Mater. Sci. EWng. 3 [1968] 189/219.
Schultz, H., Acta Met 12 [1964] 761/2.
Kornblit, L, Physica B+C 106 [1981]351/5.
W. D. Wilson, R. A. Johnson, Interatomic Potentials Simulation Lattice Defects 6th Batelle Inst. Mater. Sci. Colloq., Seattle and Harrison, Hot Springs, B.C., 1971 [1972], S. 275/90; C.A. 79 [1973] Nr. 8838.
Smedskjaer, L.C., Loper, G.D., Chason M.K., Siegel, R. W., Mater. REs. Soc. Symp. Proc. 41 [1985] 57/62.
Kornelsen, E>V>, Rad. Eff. 13 [1972]227/36.

## Slide 31: Pulsed He/Damage with Temperature Spike: