## Slide 1: Deuterium Ice Layering and Target Injection Studies
HAPL Meeting
Los Angeles, CA
2–3 June 2004
D. R. Harding
University of Rochester
Laboratory for Laser Energetics

## Slide 2: Overview
Status of ice layering effort
High-resolution images of an exploding cryogenic target
Status of thermal modeling of heat flux to IFE target
T1920

## Slide 3: Summary
High-quality (1.2-m average rms) ice layers formed in 3 hr.
There is 0.6-m variation in ice roughness due solely to the crystallizing and layering process.
Ambient radiation melts an OMEGA-scale target in 10 s and explodes it in 78 s.
  Irradiance = 0.18 mW, flux = 74 W/m2
Heat flux to cryo targets calculated for a wide range of target chamber conditions:
  1300 K and 4000 K, 100 and 400 m.s–1
  gas density = 0.03, 1.7 and 22  1021 atom/m3 (10, 50, and 700 mtorr at 300 K)
The design of equipment for measuring the efficiency of heat transfer to a cryogenic target continues.
T1931

## Slide 4: Progress continues in making higher quality ice layers. The time to form these layers is surprisingly quick
Bottom view
Top view
+y view
–y view
Y view
Y view
Y view
Y view
X view
X view
X view
4
2
0
–4
–2
Change in ice roughness during the layering process
(Cryo-2035-294)
0
40
80
120
Time (min)
0
10
20
30
rms roughness
(m)
Power (m2)
T1921
m
Side
view
Mode

## Slide 5: Four separate layers, same target, formed under “identical” conditions show repeatable topology. Variation is ±0.6-m rms
Region of thicker ice located at equator – typically where crystal initiates
Ice features not
attributable to
capsule influence
T1922
Xview
Xview
Xview
Xview
10
8
6
4
2
0
–2
–4
–6
–8
m

## Slide 6: Exploding target: 0.87-mm-diam shell; 102-m D2 layer
No evidence of bubbles
10 s to fully melt ice
78 s to explode target (measured)
Radiance on target
  0.173 mW (calc.)
14 mJ required to explode (based on time to explode and enthalpies of deuterium)
  74 W/m2
T1924

## Slide 7: High resolution images of a cryogenic target exposed to ambient radiation shows the target melting after 10 s and exploding after 78 s
To +5 s, slumping
To +76 s, gaseous
To +40 s, fully melted
To +0.25 s, still frozen
To +15 s, almost melted
T1923

## Slide 8: The vertical lineout through the target shows the gas/solid and gas/liquid interface
Ice slumping
Liquid heating and expanding
Gas fraction increasing
Rupture
60
40
20
0
–60
–40
–20
60
40
20
0
Time (s)
T1925
Normalized diameter

## Slide 9: Determining how the target will respond to the target chamber environment requires knowing the heat flux, Q (d, , T, ), on the target
Sequence
Determine approximate fluxes (heat and number) to a target. (to design experiments).
Experimentally determine the heat transfer efficiency
  What are the accommodation and sticking coefficients?
  How rapidly does Xe condense on the surface?
  Recalculate accurate fluxes
Input data as a boundary condition in a CFD model
T1926

## Slide 10: Monte Carlo simulations allow the heat flux to a target to be defined
Heat load from
  impact—need to know temperature and flux of gas striking the target
  Xe condensation (Hvaporization = 10.5 J/monolayer)— need to know number flux and rate of monolayer formation
Evaluating three gas densities
  3.2  1022 atom/m3 (0.70 torr @ 300 K)
  1.76  1021 atom/m3 (0.05 torr @ 300 K)
  3.2  1019 atom/m3 (0.01 torr @ 300 K)
Evaluating two target chamber temperatures
  4000 K
  1300 K
Evaluating two target velocities
  400 m/s
  100 m/s
T1927

## Slide 11: Monte Carlo calculations…
5 m  10 m mesh size
1-ns time steps—averaging over 2.5-s intervals
500,000 to 1,000,000 simulated molecules
Pressure distribution around the target. Range: 1 to 4 Pa
T = 4000K
Temperature distribution around the target.
Range: 500 to 4000 K
0
0.0025
0.0050
–0.0025
–0.0050
0
0.0025
0.0050
–0.0025
–0.0050
= 3 x 1019 atm/m3
 = 3  1019 atm/m3
0.005
0.004
0.003
0.002
0.001
0.000
Distance (m)
0.005
0.004
0.003
0.002
0.001
0.000
400 m/s 
Temp
Distance (m)
Distance (m)
 = 1.7  1021 atm/m3
 = 3  1019 atm/m3
Distance (m)
Distance (m)
400 m/s 
400 m/s 
T1928

## Slide 12: Monte Carlo results….
Heat transferred to target during transit (4000 K; 400 m/s)
0.00
0.01
0.02
0.03
0.04
0.05
0
1
2
3
4
5
Distance traveled (m)
Heat (J)
High density (0.7 torr): all energy transferred in
collision; no condensation
Low velocity (100m/s):
all energy lost in collision, no condensation
Worst case: all energy lost
in collision + all atoms stick
All energy lost in collision,
no condensation
Half impact energy
transferred,
no condensation
Low density (10 mtorr):
all energy lost in collision, no condensation
REFERENCE: OMEGA TARGET
* These are average values; the angular variation must also be considered.
T1929

## Slide 13: Experimental configuration
Use RHEED to measure condensation rate and sticking coefficient
Measure the rate deuterium ice melts to determine accommodation and sticking coefficients
T1930
Ion beam (<1 ev) OR pulsed molecular beam
Xe
1 atm
RHEED
1300 K
Orifice
10  100 m
1000 /s
1000 /s
Detector
18 K cryo
target or
temperature
sensor
100-m diam spot
T gas ~ 900 K
1023 to 1025
atm
m2 • s
1017 to 1019
atm
s
Flux

## Slide 14: Summary/Conclusions
High-quality (1.2-m average rms) ice layers formed in 3 hr.
There is 0.6-m variation in ice roughness due solely to the crystallizing and layering process.
Ambient radiation melts an OMEGA-scale target in 10 s and explodes it in 78 s.
  Irradiance = 0.18 mW, flux = 74 W/m2
Heat flux to cryo targets calculated for a wide range of target chamber conditions:
  1300 K and 4000 K, 100 and 400 m.s–1
  gas density = 0.03, 1.7 and 22  1021 atom/m3 (10, 50, and 700 mtorr at 300 K)
The design of equipment for measuring the efficiency of heat transfer to a cryogenic target continues.
T1931