## Slide 1
Progress of Mass Production Studies for IFE Targets
Brian Vermillion, Barry McQuillan, Lloyd Brown, Dan Goodin, Haibo Huang, Patrick Goodman, Willa Maksaereekul, Jon Streit, Diana Schroen
High Average Power Laser Program Workshop
Los Angeles, California
June 2-3, 2004

## Slide 2
Topics
  Our Objective:
  Develop mass production methods for IFE targets, identifying the processes to increase from laboratory scale to 500,000 plus targets per day
  Since the last HAPL meeting, we have been addressing the issues of:
    Continuous flow apparatus for mass production of the Divinylbenzene/Polyvinylphenol, DVB/PVP, foam capsule
    Capsules sticking together during the polycondensation reaction stage
    CO2 critical point drying and dehydration fluids
    PVP overcoat bonding to DVB foam
    Scaleup and process control

## Slide 3
    A flow through tube design decreases the amount of handling to which a capsule is subjected
    Counter current fluid exchange can be utilized throughout the continuous flow process, utilizes porous Teflon to facilitate fluid exchange
      Washing steps for switch to PVP chemistry from DVB chemistry
      Dehydration before CO2 drying: Water to IPA
We are applying counter current fluid exchange methodology
10 L/h 100% IPA
10 L/h 80% IPA
10 L/h 90% IPA
10 L/h 70% IPA
10 L/h ~ 100% IPA
10 L/h 70% IPA

## Slide 4
    Propose apparatus to control shell separation
    High pressure drop tubing creates a smooth inlet of fluid into the main flow stream, separating the capsules
We are developing methods to prevent sticking of capsules during the PVP condensation reaction
Porous Teflon tubing high pressure drop
10 L/h Water
20 L/h solution
Hard DVB shells
10 L/h PVP solution

## Slide 5
    Counter flow column design uses stages
    Applicable at “non-sticking” stages and for large quantities
    Originally designed for ceramic fuel particle extractions
Counter flow column may also be useful for extractions
10 L/h 80% IPA
10 L/h 90% IPA
10 L/h 100% IPA
10 L/h ~70% IPA
10 ~ 100% L/h IPA
Dilute IPA out to reprocessing
Dilute IPA out to reprocessing
Dilute IPA out to reprocessing
Industrial System

## Slide 6
    Why use CO2 critical point drying?
      We use CO2 to remove solvent and dry the targets without damage resulting from surface tension change from exposure to a gas-liquid interface
    Most commercial units designed for semi-conductor or food industries
      Controlled process variables for these units are not ideal for foam capsule mass production
        Dilution of solvent is generally not quantized
        Pressure control is rough
        Size is optimized for specific industrial needs: Not designed for large quantities of IFE targets
Controlled CO2 critical point drying is necessary
Laboratory Scale System

## Slide 7
    Working on a scaleup dryer unit
      Larger volume, one section can handle thousands of capsules
      Pressure (~1.2 Ksi), temperature (~50ºC), and release rate of CO2
      Improved process control/repeatability
      Quantity of CO2 used for each batch
        Study how solubility of liquid and supercritical CO2 affects capsule production
      Design underway, major components identified
    Examining different dehydration solvents for last fluid exchange
      Currently IPA
      Dioxane used previously, but has toxicity issues
      Maybe diethylphthalate, DEP, which might provide a smoother overcoat as well
Examining a scaled up CO2 dryer design and last fluid exchanges before CO2 drying
Scaleup dryer unit diagram
12 in tall
4 in ID
Sieve trays with capsules
Pressure Vessel

## Slide 8
    As mentioned, working towards a continuous flow apparatus to increase production of capsules
    System would finish with batch process CO2 dryers operating in parallel
Let’s put it all together!
Washes/Exchanges
Condensation Reaction
CO2 Extraction
DVB foam capsules
    System would switch back to semi-batch mode during critical point drying
    Continuous flow apparatus most likely not required for this stage

## Slide 9
    As the overcoat forms, data indicates it has a tendency to form outwards from foam pores
    Likely a result of PVP polymer chain cross linking, preventing remaining PVP from getting through
    Loose overcoat may lead to the following:
      Poor gas retention
      Low yield
      Blistering during chamber injection
    Examining a method to improve linking of PVP overcoat onto DVB foam capsule by growing the full density overcoat inwards
Examining condensation chemistry to better attach CH full density overcoat to DVB foam shell
IPT
PVP
DVB Foam Tendril
Water/Oil Interface
Time
C
OH
OH
C
C
PVP unit
1
2
3
4
5
6

## Slide 10
    We are evaluating growing the full density overcoat into the pores of the DVB foam by changing from PVP to Bisphenol-A
    Bisphenol-A forms long tendrils, may allow additional Bisphenol-A to get deeper into foam wall
    Past experimentation by M. Takagi, now need to examine with renewed focus
Let’s grow the layer inwards
Fragile bond
low yield
More stable
higher yield
DVB foam
Overcoat (3-5 µm)
C
CH3
CH3
OH
OH
    Additionally, a two monomer system may be desirable to increase smoothness
    Switch back to PVP after initial “bonding layer” has been formed with Bisphenol-A
    Testing underway
Bisphenol-A unit

## Slide 11
Applying process control to IFE foam target production
  Testing apparatus to measure process variables
  Currently using point laser source-photo sensor diode pairs
  System is fast in real-time, can be used for control feedback
DAQ
Lasers
Sensors
Real Time Feedback
Mass Flow Control
  Lasers
  Class IIA, 0.5 mW
  2 PSDs
  1.2 (mm2) active area
  2 Photocurrent amplifiers
  DAQ
  PCI DAQ card
  LabView VI

## Slide 12
Apparatus successfully images clear uncured polystyrene capsules
  Initial bench test runs completed
  Modifying LabView VIs for real-time data analysis
  Plan to test a planar source to ensure coverage of flow tube and consistent results
  Opaque DVB foam shells should be easier to acquire than polystyrene!

## Slide 13
System can provide the means for many process control studies
  Data analysis from this run
  Average rate: 0.29 s
  Standard Deviation: 0.05 s
  Other process variables or results that might be determined with this system
  Diameter, wall thickness, out-of-round, non-concentricity, capsule separation
  Formation of beads (loss of encapsulation), satellites (debris left from droplet formation)

## Slide 14
Sensor system can be used for additional studies
    Study variables that control non-concentricity
      Many sensor pairs mounted in the proposed continuous flow tube apparatus
    Speed of gelation for DVB shells

## Slide 15
Image analysis as a tool for more advanced process control and real-time characterization
Propose using still image analysis for diameter and out of round
  Blob analysis correlation to wet and dry diameters
  Wet capsule calculation for OD: OD = ID x (1+O1/W1)1/3
  Wet capsule calculation for ID: ID = ((W1 x 6) / (3600 x π))1/3
  Dry capsule correlation for polystyrene: OD=ID x (1 + f(O1)/W1)1/3
  Where: OD = Outside Diameter
  ID = Inside Diameter
  O1 = Oil Phase
  W1 = Inner Water Phase
  f(O1) = wt% polymer in Oil Phase
  For DVB foam capsules, we start with wet shell calculations, no loss of solvent, but realize this is just an approximation
  Studies underway to determine empirical correlations between wet and dry targets
  Working with National Instruments to determine capabilities for real-time characterization utilizing Vision Analysis software

## Slide 16
Brief Status of Target Layering Experiment (Cryogenic Fluidized Bed)
One target systems are highly isothermal for short times
This system would be highly isothermal time-averaged
Spec out to vendor as a package:
  Vacuum shell, thermal shield, manipulator, stand, lift mechanism for shell
GA will build/procure
  Flow loop - includes: fluidized bed, helium blower, …
  Heat exchangers, cryocoolers, permeation cell
Updated flow loop for reversible flow (per UR/LLE comments)
PR out to Barber-Nichols
Long lead item (6 months)

## Slide 17
Near term work plans
    Continue development of counter current fluid exchange apparatus, including the PVP condensation reaction stage
    Continue design and test the scaleup CO2 dryer
    Examine last fluid exchanges of capsule drying to improve yield
    Complete studies for improved full density overcoat
    Continue development of sensor system for process control (switch to planer source)
      Perform additional modifications to study:
        Shell rate of formation
        Diameter
        Non-Concentricity
    Work with NI to determine best course for image analysis and apply towards real time characterization

## Slide 18
Summary and Future Considerations
    Summary
    Started design of a continuous flow apparatus for mass production of the DVB/PVP, foam capsule, including apparatus to prevent capsules sticking together during the polycondensation reaction stage
    Designing a CO2 critical point drying for larger scale operations
    Examining PVP overcoat chemistry to improve bonding
    Designed, fabricated and tested a system to quantify capsule rate of formation, working towards the goal of scaleup and process control for mass production
    Future Considerations
    Surface smoothness, gas retentiveness and buckling pressure of DVB/PVP targets
    Cryogenic study of target
    Real-time characterization study
      Identifying correlations between wet and dry capsules
      Example: RF foam shells demonstrate about a 5% shrinkage from wet to dry, what is it for overcoated DVB?