## Slide 1: Progress on the Development of a Unified Materials Response Code (UMARCO)
Nasr M. Ghoniem (UCLA)
for
Qiyang Hu, Mike Andersen, Shahram Sharafat (UCLA), Akiyuki Takahashi (Kyoto), Jake Blanchard (UW)
Notes: <number>

## Slide 2
Traditional approach:
Unified Materials Response Code (UMARCO):
Inputs:
  Threats
    Ion spectra
    X-ray spectra
    Neutron spectra
    Laser intensity
  Properties
Outputs:
  Implantation profiles
  Heat deposition
  Temperatures
  Stresses & Strains
  Crack nucleation & roughening
  Crack propagation
  species concentrations
  Bubble concentrations
UMARCO
Thermo-structural Models
Ion Effects Models
HAPL Chamber Analyses
Exposure Experiments
Thermo-mechanical Response: Q. Hu, J. Blanchard
Notes: <number>

## Slide 3: Progress Overview
Last meeting:
  Ion implantation in W
  Heat generation in W
  Elastic and perfectly-plastic mechanical response in single shot
This meeting:
  Work hardening plastic response in single shot
  Multiple shots -> cyclic plasticity
  Ion implantation in SiC
  Heat generation in SiC
  Elastic and perfect plastic response of SiC
  Surface Roughening in elastic materials
  Surface Roughening & crack nucleation in elasto-plastic materials
Notes: <number>

## Slide 4: Stress Analysis: (with work-hardening)
For tungsten:
E = 411GPa,  = 0.28
 = 4.510-6 /K, yp= 750 Mpa, Et=9 Gpa, T=2600 C (fixed)
xx
yy
E
Et
RT
1750 C
2800 C
2600 C
Notes: <number>

## Slide 5: Single shot on W: stress & strain on surface
Notes: <number>

## Slide 6
Multiple Shots: cyclic plasticity

## Slide 7: Multiple Shots
Notes: <number>

## Slide 8: Stress & Strain through the depth
Notes: <number>

## Slide 9: Inertial Effects on Stress State due to Elastic Waves Produced by Rapid Heating
Notes: <number>

## Slide 10: Ions in SiC: stopping power calculation
SiC | H | D | T | He | C
A | 6108.6 | 8825.8 | 28017 | 187761 | 8.35E9
B | 140.08 | 299.87 | 1172.8 | 5377.8 | 1.36E8
C | 0.4523 | 0.3574 | 0.7833 | 1.0438 | 8.74E2
D | 0.088 | 0.063 | 0.0477 | 0.1041 | 8.7E-4
Brice Formulae:
C
H
He
T
D
Using Perkin’s ion spectra, fitting SRIM data with the model, we can solve from Excel:
Notes: <number>

## Slide 11: SiC vs. W: Ion profiles & Surface heating
Notes: <number>

## Slide 12: SiC mechanical response: @ Surface
Notes: <number>

## Slide 13: SiC mechanical response: through depth
Elastic
Plastic
Notes: <number>

## Slide 14
Surface Crack Nucleation without Plasticity
Surface Roughening & Crack Nucleation: M. Andersen & A. Takahashi
Notes: <number>

## Slide 15
Surface Crack Nucleation including Plasticity
Notes: <number>

## Slide 16
W High T Properties
E: 390 GPa
: 0.28
: 2.6 J/m2
D: 1e-14 cm2 / s
Time to reach critical crack depth
  Perfectly Plastic: 49 s – depends on value of D
    Continuous loading at yield stress, 550 MPa.
  Hardening: 25 s
    Loading is increased to 734 MPa.
Initial roughness on the order of 10 nm.
J.F. Latkowski, JNM 2005.
Notes: <number>

## Slide 17
Roughening model produces surface profile similar to experimental results.
T.J. Renk JNM 2005.
Critical depth reached after 49 seconds.
Notes: <number>

## Slide 18
b
b
70.5o
Super-dislocation containing 100 dislocation and 100 x Burgers Vector.
Curvature as a function of time.
Blunting effect shown by drop in curvature.
Notes: <number>

## Slide 19: Future Directions – Thermo-mechanical Modeling
W Thermo-mechanical Model:
  temperature-dependent yield surface;
  general work-hardening;
  Stress Intensity Factor & Propagation of Cracks.
  Inertial Effects with Plasticity.
SiC Thermo-mechanical Model
  Include realistic Model of Surface Fracture
  Statistical Model of SiC Fracture (depends on Processing)
Model Extensions to RHEPP, DragonFire, and to New Spectra
Notes: <number>

## Slide 20: Future Directions - Roughening
Calibrate Surface Diffusion with Experiments:
  Measure Ds directly
  Measure average roughening per pulse.
Dependence of Final Roughness on Initial Surface Conditions
Dependence of roughening velocity on grain boundary versus bulk properties.
Notes: <number>