## Slide 1: Progress in Mass Production Layering Demonstrations
Presented By
Neil Alexander1
Don Bittner2, Kurt Boehm3, Landon Carlson1, Dan Frey1, Dan Goodin1, Jim Kulchar1, Ron Petzoldt1, Robert Stemke1 and Emanuil Valmianski1
HAPL Meeting
Naval Research Laboratory
Washington, DC
October 30 – 31, 2007
1: General Atomics
2: Schafer
3: UCSD

## Slide 2: Fluidized bed for layering is operating at cryogenic temperatures
Accomplishments since last report when layering cryostat was delivered and being outfitted
Fluidized bed successfully operated at <10 K
  Au/Pd coated PAMS shells
  Static cling overcome at cryogenic temperature
    Polonium source
Cryogenic vacuum chuck successfully captured targets
  Will allow still target characterization
Surface roughening reduced at cryogenic temperature
Notes: ***Remember to say for last bullet that that previous WYKO measurements showed that there was roughing increase over time at room temperature, but that is was below spec for 13 hr layering and unload time

## Slide 3: Cold plant, cryo blower, and fluid bed were added to layering cryostat (MPLX)
Vacuum vessels removed for clarity
Bed fluidizing at cryogenic temperatures…
Helium In
Helium Out
Vacuum Chuck Line
Fluid Bed

## Slide 4: Video shows fluidization at 11 K and capture of target with vacuum chuck
Bed fluidized as low as 9 K
We have run it for days at a time
Vacuum Chuck needle
Au/Pd coated PAMS capsules
Helium flow
Polonium strip below frit
Frit
17 x reduced speed
Vacuum needle tip will capture target
Bed at 11 K

## Slide 5: Previously, we reported roughness measurements
WYKO roughness measurements showed <50 nm at 16 hour
  Room temperature bed
roughness spec
16 hr. estimated time in bed for power plant
2mm OD, 200 Å Au-coated shells
Bed expansion of 2
Five shells pulled periodically

## Slide 6: Au/Pd layer roughening reduced at cryogenic temperature
0.4 µm GDP overcoat on Au/Pd Layer
Cryogenic Temperature
16 hours in 2x bed represents layering and unloading time
Au/Pd coating pull-outs, so very shallow, ~30nm
GDP micro-coat also reduces roughening
Au/Pd layer
Room Temperature
0.6 µm GDP overcoat on Au/Pd layer
Room Temperature
Au/Pd
Cryogenic Temperature

## Slide 7: As point defects pullouts are smaller than what the NIF spec considers noteworthy
Area loss in reflective coating does not add significant heat to DT layer
  GDP overcoat on Au/Pd +4% heat flux
IR absorption in 0.3 µm overcoat GDP would add +7%
Slight GDP overcoat adds little heat to DT layer
  4%+7%=+11%
GDP chips, Au/Pd pull-outs
GDP overcoat okay?
Are there other effects to consider?
Isolated defect NIF point design spec

## Slide 8: Kurt Boehm has developed a fluidized bed model/simulation
Tracks individual target trajectories and spins
  Each target has a unique moment of inertia tensor
  Tracking of temperature of target on its trajectory will be added
Target trajectories through bed temperature field will be used to predict layer quality
Will provide a design tool for power plant layering beds

## Slide 9: Bed model is being bench marked to experiments and bed correlations
Model is correlating well with experiments

## Slide 10: Ready to proceed to cryogenic layering, injection, tracking
Short term plan:
  Layering experiment
    Permeation filling, Optical characterization
Long term plan:
  Removal of targets from bed
  Transfer layered targets to cryo injector
  Characterize layered targets after injection
    Oven on flight tube
    Gated image in flight
  Tracking and engagement of cryo layered target