## Slide 1
Global Performance Statistics
Introduction
Mechanical
Properties
Summary
Thermo-Structural
Analysis
Hibachi Foil Geometry
Test Temp. & Condition | E (GPa) | Etan (GPa) | Yield (MPa) NRL Data
21 oC as received | 39.16 | 2.26 | 310
21 oC exposed | 36.82 | 1.27 | 434
400 oC as received | 12.59 | 3.29 | 209
400 oC exposed | 17.22 | 8.41 | 365
Young’s Modulus (E) and Tangent
Modulus (Etan) estimated based on
NRL data.
Shell elements used for elastic and
plastic analysis.
Temperatures:
Tfoil ≈ 180˚C - 450˚C
Δtfoil ≈ 30˚C (swing/shot)
Laser Gas Pressure:
P ≈ 20 psi (0.138 Mpa)
Times:
f = 5 Hz
Δ ≈ 140 ns (heating)
Δ ≈ 10 μs (mechanical)
For runs: 5/13/2004 to 1/16/2008
447,963 shots
63 different foils
33 foil failures
18 failures due to holes
15 failures due to “blows”
Max: ~25,000 shots (no wrinkles)
Foil Characteristics:
Stainless steel 304
Temper: ANN
Finish: 4F
Thickness: 0.001 in (25 μm)
Foil is pinhole free, and appears to have uniform thickness within 2%
In-situ stress-strain measurements
show more consistency than professional data
Four Models:
  Flat Foil
  Curved Foil
  Flat Foil & Curved Support
  Scalloped Foil
Analysis
Shell Elements
Pressure
Thermal
Pressure +Thermal
Linear/Non-linear
FEM analysis is performed on a variety of geometrical models and analysis types using ANSYS Multiphysics and COSMOSWorks.
Model 4: Scalloped
Thermo-mechanical Analysis of the Hibachi
Foil for the Electra Laser System
A. Aoyama1, J. Blanchard2, J. Sethian3, N. Ghoniem1, and S. Sharafat1
1University of California Los Angeles, Los Angeles, CA
2University of Wisconsin, Madison, WI 3Naval Research Laboratory, Washington D.C.
A single foil section is modeled flat
Pressure Only:
With all four outer edges held fixed, and pressure applied, model deforms elastically.
Model 1: Flat Foil
Stress
smax ~ 340 MPa
Displacement
dmax~3 mm
Strain
emax~0.05
Pressure and Temperature Loading Applied:
Addition of thermal loading creates ripple effects running parallel to width of foil.
Geometry:
To further examine the high strains along edges, a surface with pre-loading curvature (only along the width) was modeled under the same loading conditions.
Model 2: Curved Foil
B. Pressure and Temperature Loading
In this case, the “wrinkle” caused by thermal expansion is very localized.
Is the foil buckling?
Plastic strain contours
7 mm
Cross-section view
An conservative eigenvalue buckling analysis was performed to determine an approximate first buckling mode.
From this preliminary analysis, it appears that under temperature loading, when the foil buckles, the largest deflections are near the ends.
C. Static Buckling Analysis
Displacement
(magnitude) contours
Analysis Modes Performed:
Pressure Loading Only
Pressure And Temperature
Static Buckling
Non-Linear Buckling
Geometry:
This analysis examined the effects of curving the supports that hold the foil in place.
This is done to attempt to alleviate the very large rotations of the foil about the long edges.
Front View
It is immediately apparent that the shape of these rigid supports ease the transition to the foil’s equilibrium state.
Model 3: Flat Foil + Curved Rib
Compared to the original flat model (Case 1) with a similar mesh density, we see a significant decrease in plastic strain.
Original Flat Foil
With Curved Supports
Max Plastic Strain: 0.039
Max Plastic Strain: 0.016
Original Geometry:
This analysis examined the effects of curving the supports and curving the foil.
J Parish, CTI Inc. 2008
Details of the Scallops
FEM Model:
This non-linear analysis assumes the foil can slide on the curved rib (tough analysis small section is modeled with symmetry BC, 1064 elements).
Effects of end foil end geometry is absent, which plays an important role in the stress state
Four Models were investigated:
  Flat foil
  Curved foil
  Flat foil & curved support
  Scalloped foil
  Pressure + Thermal loads of (1) shows wrinkle formation
  Pressure + Thermal load of (2) inconclusive (pressure alone shows ½ strain of flat; wrinkles using non-linear buckling)
  Pressure (only) of (3) shows ½ strain of flat
  Pressure (only) of (4) shows:
Effects of thermal load and “end-geometry” for scalloped foil remains to be analyzed
  Max. Displacement factor of 100 less than (1)
  Max. Stress factor of 2 less than (1)
  Max. Plastic strain ~100 X less than (1) and 40 X less than (2) and (3)
A. Pressure Loading Only
With all four edges fixed, and pressure applied, the model deforms elastically.
Displacement (magnitude) contours
Von Mises Stress Contours
A more conservative approach is to use
a nonlinear buckling analysis.
In this case, the temperature load is
increased until the solution begins to
diverge.
Then, an ANSYS nonlinear stabilization
option adds an artificial damper to maintain a stable state.
The damping coefficients are tracked and are used to make corrections to the results.
Displacement (magnitude) contours
D. Non-Linear Buckling Analysis
Plastic Strain Contours
Displacement Contours
Factor 100 smaller from flat model
Factor  70 smaller from flat with curved ribs
Foil slides on
curved structure
(graphical artifact
of thin shell elements)
The shape of these rounded supports and rounded foil ease the transition to the foil’s equilibrium state resulting in small deformations  30 mm
Stress Contours
Foil slides on
curved structure
(graphical artifact
of thin shell elements)
Max. stress  170 MPa along the edge Foil stress fairly uniform
With this geometry, and only pressure applied, the foil deforms elastically.
Foil slides on
curved structure
(graphical artifact
of thin shell elements)
Max Plastic Strain  0.0005 along the edge
This is done to attempt to further alleviate the rotations of the foil about the long edges.
J Parish, CTI Inc. 2008
  Factor of  80 less from flat foil,  40 curved foil and flat foil with curved structure
Strain Contours
Residual Stress: Unload
from 26.6 psi
to 0 psi
Residual stress levels are
low: 0.065 MPa
(pressure only)
At max. pressure: 26.6 psi
5 Cycles at 400 oC:
Stress ~ 340 MPa
Strain ~ 3.9 % (max along rib edges)
Stress
Strain
In support of the High Average Power Laser (HAPL) project the Electra Laser, a KrF Gas Laser system is being developed at NRL.
Laser uses high voltage (500-800 keV), high current (100-500 kA), short pulse (100-600 ns) electron beam
Electron beam pumps 0.14 MPa pressurized KrF gas cell
Gas cell is separated from the vacuum region by a 25 μm-thick stainless steel (SUS304) foil, the Hibachi Foil
Foil operates between 180 °C and 450 °C
Typical foil dimensions are about 0.3 m x 1.0 m
Laser pulses at up to 5 Hz, subjecting foil to repetitive thermal and mechanical stresses
Foil experimentally lasts 1,000-20,000 shots before failure
Various design modifications are being considered to improve foil performance
In this study we report on the comparative thermo-mechanical analysis between different foil geometries
It is demonstrated that the scalloped design
reduces stresses to within yield limits of the
SUS304 material