
A “PCA” version of 304 SS

for thick flibe protected walls

300 series for fluoride corrosion (TF+T2) resistance by its Ni

316 SS modified became radiation resistant PCA 

(Prime Candidate Alloy)

But its Mo and Nb causes high level waste

Can 304 SS (absence of Mo and Nb) also be modifed?


R. W. Moir-LLNL

Phil Maziasz-ORNL

Nate Hoffman-Consultant, LLNL
ARIES project Meeting

Hilton Garden Inn

2801 Constitution Drive, Livermore, CA

May 6, 2003

316 SS was successfully modified with Ti and other elements to reduce swelling to become PCA [image: image1.wmf]
PCA is not as low swelling as some other materials but might be adequate. [image: image2.png]SWELLING, %

PCA-CW
(450-550°C)






304 SS can likely also be Ti modified becoming “PCA” 304 SS with adequate radiation damage resistance.


316 SS
316 PCA
304
304 “PCA”

Fe
70
65
70
~68

Cr
16-18
14
17-19
18

Ni
12-14
16
10
13

Mo
2.5
2.3
<0.5
trace

Mn
2
1.8
0.7
1-2

Nb
0.01
0.01

trace

V

0.005
0.005
0.5 max

W

0.01

3 max

Ti
0.005
0.24

0.3-0.4

C
0.05
0.05

0.08 ?

P
<0.02
?

0.03 to 0.07

B
<0.001
?
<0.001
0.005 to 0.01

Si
0.5-1.0
0.5
0.4-1.0
0.5 to 1

                      = important addition                               trace     = cost limited
Conclusions:

An alloy development program with fission reactor testing likely can come up with a “PCA” like version of 304 SS. 100 dpa and adequate ductility might be achievable for use behind 0.5 m of flibe as a structural material at ~650 °C.

That is, modest modifications to an existing material might be useable with minimal development and retain its nickel based robustness to fluoride corrosion.

Best swelling data should be on modified PCA alloys and on French 15/15TiSi alloys.  see P.J. Maziasz, Journal of Nuclear Materials 205 (1993) 118-145.

[image: image3.png]A Gy (kcal/mole F,)

Temperature, K

2000

3000




[image: image4.png]AGy (kcal/mole F )

| 1000
900

Temperature, K



















