## Slide 1: Fracture of Divertor Structures
Jake Blanchard
ARIES Meeting
April 2011

## Slide 2: Outline
Primer on Fracture Mechanics
Preliminary Results for Divertor Structures
Future Plans

## Slide 3: Design of Engineering Structures
In early 20th century, design of metal structures was strictly stress based
Onset of high performance ships (Liberty ships, WWII) changed things

## Slide 4: What happened?
stress
Temperature
fracture
Low strength
high strength

## Slide 5: Fracture Mechanics
Size and Orientation of Cracks
Stress Fields
Material Properties

## Slide 6: Crack Tip Stress Fields (Elastic)
Consider a sharp crack in an elastic material
K is stress intensity factor
Function of geometry and loading
Fracture occurs when K reaches critical value (KIC – fracture toughness)
r


## Slide 7: An Example
Consider an infinite plate with a through crack
Glass: KIC=1 MPa-m0.5
Al: KIC=20 MPa-m0.5
For a=100 microns, fracture stresses are 56 MPa for glass and 1,100 MPa for Al

## Slide 8: Fracture Toughness (room temp)
Material | Toughness (MPa – m^0.5)
7075 Aluminum | 24
4340 Steel | 50
Silicon Carbide | 4
Polystyrene | 1
Tungsten (polycrystalline) | 5
Beryllium | 10
These values depend strongly on processing.

## Slide 9: Ductile vs. Brittle

## Slide 10: Temperature Dependence

## Slide 11: Stress Fields in Ductile Materials
Ductile materials will develop plastic deformation at crack tips
This toughens material and resists catastrophic crack growth
Previous analysis is not valid
Analysis uses integral around crack tip, rather than stress intensity factor

## Slide 12: Failure Criterion for Ductile Materials
Base failure prediction on work required to create fresh fracture surface
Write as line integral
W=strain energy density
T=tractions
U=displacement

## Slide 13: Irradiated Materials

## Slide 14: Fatigue Crack Growth
Previous analyses refer to catastrophic, unstable crack growth
Repeated application of loads can lead to incremental crack growth

## Slide 15: Characterizing Cracks
Key Question: What is initial crack size?
We need non-destructive examination (NDE)
Options:
  Dye penetrant
  Ultrasound
  X-rays
  Eddy currents
  Thermography
  Etc.
Costs and capabilities vary

## Slide 16: ITER Structural Design Criteria
Primary Loads
Primary + Secondary Loads
Elasto-Plastic Analysis

## Slide 17: ANSYS Finite Element Model of Circumferential Crack
Crack face
Stress intensities along crack face using the ANSYS CINT command
Elastic-Plastic material properties for Tungsten used
Currently only pressure loads are considered, but thermal stresses to be included

## Slide 18: Initial Fracture Studies Based on T-Tube Geometry and Pressure Loads
t = 1 mm
OD = 15 mm
Coolant pressure ~ 10 Mpa
Coolant inlet temperature ~ 600 oC
Tungsten

## Slide 19: Initial Studies Compute Stress Intensities for Axial Cracks in Pressurized Cylinder
Case 1: Circular crack; c/a=1
Case 2: Elliptical crack; c/a=2
Use elastic-plastic properties
for tungsten.
Calculate J1 and then report
equivalent KI.

## Slide 20: Variation of Stress Intensity with Location along Crack Tip (a = 0.1 mm)
f
Case 1: Circular crack; c/a=1
Case 2: Elliptical crack; c/a=2
a = 0.1mm
Chart: f (degrees)
| 0 | 2.25 | 4.5 | 6.75 | 9 | 11.25 | 13.5 | 15.75 | 18 | 20.25 | 22.5 | 24.75 | 27 | 29.25 | 31.5 | 33.75 | 36 | 38.25 | 40.5 | 42.75 | 45 | 47.25 | 49.5 | 51.75 | 54 | 56.25 | 58.5 | 60.75 | 63 | 65.25 | 67.5 | 69.75 | 72 | 74.25 | 76.5 | 78.75 | 81 | 83.25 | 85.5 | 87.75 | 90
cylindrical | 0.9322 | 0.9595 | 0.9575 | 0.9512 | 0.9519 | 0.9516 | 0.9522 | 0.9525 | 0.9531 | 0.9537 | 0.9544 | 0.9552 | 0.9562 | 0.9572 | 0.9584 | 0.9597 | 0.961 | 0.9626 | 0.9642 | 0.966 | 0.968 | 0.9701 | 0.9725 | 0.9751 | 0.9779 | 0.981 | 0.9844 | 0.9881 | 0.9923 | 0.9968 | 1.002 | 1.0075 | 1.0142 | 1.021 | 1.0298 | 1.0383 | 1.05 | 1.06 | 1.0801 | 1.0897 | 1.0515
elliptical | 1.2484 | 1.2608 | 1.2592 | 1.2553 | 1.2539 | 1.2518 | 1.2496 | 1.2469 | 1.244 | 1.2407 | 1.2371 | 1.2332 | 1.2289 | 1.2243 | 1.2191 | 1.2137 | 1.2077 | 1.2014 | 1.1945 | 1.1874 | 1.1797 | 1.1718 | 1.1633 | 1.1545 | 1.145 | 1.1353 | 1.1251 | 1.1145 | 1.1037 | 1.0926 | 1.0816 | 1.0706 | 1.0607 | 1.051 | 1.0444 | 1.0385 | 1.0404 | 1.0421 | 1.0789 | 1.1051 | 1.0006

## Slide 21: Maximum Stress Intensity as a Function of Crack Depth
Chart: Crack Depth (mm)
| 0.05 | 0.1 | 0.2 | 0.30000000000000021 | 0.4 | 0.5
Cylindrical | 0.76 | 1.09 | 1.54 | 1.91 | 2.24 | 2.57
Elliptical | 0.88 | 1.26 | 1.78 | 2.21 | 2.62 | 3.01

## Slide 22: Conclusions
We’ve got to include fracture in our design analysis, particularly when using materials with limited ductility
So far, there are no major red flags
We will include thermal stresses in the future