## Slide 1: Update on Fracture Analyses
Jake Blanchard
July 2011

## Slide 2: Outline
2-D Analysis of Flat Plate Divertor
  High stress areas
  Crack locations
  Thermal stress included
  Consider full power and cool-down
Future Work
Conclusions

## Slide 3: Last Time We Analyzed This Design
t = 1 mm
OD = 15 mm
Coolant pressure ~ 10 Mpa
Coolant inlet temperature ~ 600 oC
Tungsten

## Slide 4: Here We Switch to Plate-Type Divertor
Tungsten HCFP(Helium-cooled Flat Plate) divertor

## Slide 5: Temperature Distributions Simulated Using ARIES Design Loads with Simplified Convection Cooling
q”=11 MW/m2
q’’’=17.5 MW/m3
P=10 MPa
Tcoolant=600 ᵒC
Max. Tarmor= 2000 ᵒC
Max. Tstructure=1310 ᵒC
Min. Tstructure=725 ᵒC
2-D Planar models are used in these preliminary studies (simulating long cracks)
Convection coefficients adjusted to correlate with ARIES CFD results
Studies show fracture results insensitive to small changes in temperature
oC
Convection

## Slide 6: Structural Boundary Conditions Adjusted to Not Over-Constrain Model
symmetry
Surface must remain planar but my rotate
Planar rotations in x-direction simulate panel bow
Results calculated with both plane stress / plane strain assumptions in z-direction

## Slide 7: Analysis of Uncracked Structure Identified Two Areas of High Stress
Max. Compressive Stress
Max. Tensile Stress
Crack Stress Intensities investigated for regions of max tensile and compressive stresses
Region of max compressive stress has tensile stress at cool down due to plasticity
Equivalent Stress (MPa)
X-Direction Stress (MPa)

## Slide 8: Crack on Internal Surface of Outer Wall
Chart: Crack Depth (mm)
| 5.000000000000001E-2 | 0.1 | 0.2 | 0.3000000000000001 | 0.4 | 0.5
Plane strain | 10.4 | 14.2 | 19.3 | 23.4 | 27.3 | 30.7
Plain Stress | 12.285 | 16.107 | 21.294 | 25.571 | 29.302 | 32.487
Crack face
Max stress intensity occurs when hot
Plane stress / plane strain assumptions give similar results

## Slide 9: Fracture Toughness of Tungsten
This is just a representative data set

## Slide 10: Crack on External Surface of Outer Wall
Chart: Crack Depth (mm)
| 0.05 | 0.1 | 0.2 | 0.3000000000000001 | 0.4 | 0.5
Plane strain | 16.5 | 19.2 | 21.7 | 23.7 | 25.7 | 27.9
Plain Stress | 6.348 | 6.164 | 4.692 | 4.876 | 5.612 | 6.532
Max stress intensity occurs after cool-down
Plane stress / plane strain assumptions give radically results – full 3-D model required, but results should be closer to plane strain

## Slide 11: Future Work
3-D fracture models
Cracks in “Tiles” and elsewhere
Try to clarify appropriate toughness data for failure analysis

## Slide 12: Conclusions
For this design, stress intensity is highest on inner surface at full power
Stress intensity is also quite high at outer surface on shutdown
It appears that permissible crack depths will be less than 50 microns
3-D analysis, toughness review, and review of NDE capabilities are needed to make concrete design recommendations