## Slide 1: Possibility of the He-Cooled SiC-Composite Divertor
X.R. Wang1, S. Malang2, M. S. Tillack1
  1University of California, San Diego, CA
  2Fusion Nuclear Technology Consulting, Germany
ARIES-Pathways Project Meeting
Gaithersburg, MD
July 27-28, 2011

## Slide 2: Outline
Review of the ARIES SiC-composite divertor designs
  Helium-cooled small SiC-composite tube divertor for ARIES-I (1991)
  LiPb-cooled SiC-composite plate divertor for ARIES-AT (2000)
Update on the SiC composite properties and design window since ARIES-AT
Possibility of using SiC composite as divertor structural material with an impinging-jet-cooling scheme
  an ARIES-finger with modifications (semi-circular thimble)
  an original ARIES-finger (W thimble/channel replaced by SiC-composite)
  a larger SiC-composite tube with impinging cooling method
Summary

## Slide 3: He-Cooled SiC/Sic Divertor of ARIES-I Was Designed to Remove a HF up to 4.5 MW/m2*
*F. Najmabadi et al., “The ARIES-I Tokamak Reactor Study”, Final Report, 1991.
ARIES-Divertor target Configuration
Schematic of the ARIES-I layout
Attractiveness of SiC/SiC in fusion application:
  elevated temperature strength,
  chemical stability,
  low activation / low decay heat
  low thermal expansion
Issues
  swelling under irradiation,
  fabrication and joints,
  stress limit

## Slide 4: Pumping Power Was Larger than 10% in order to Meet Temperature and Stress Limits
Tinlet =350 ᵒC, Texit =650 ᵒC
P=10 MPa, v=150 m/s
q”peak=4.5 MW/m2, qv=23 MW/m3
HTC=12.9 kW/m2-K
Pp/Pth =12%
Ts<1000 ᵒC
Tube d=2.5 mm
Thickness t=0.5 mm
σp+th < 190 MPa
2 mm W Coating
σp=86 MPa
Tinterface=700 ᵒC
Tmin=399 ᵒC
Tmax=776 ᵒC
CVD: chemical vapor deposition
CVI: chemical vapor infiltration

## Slide 5: Stress Limit of the SiC/SiC Used in ARIES-I &AT Is Very Conservative Assumption
Density | 3.2 g/cm3
Young’s modulus | 200-300 GPa
Poisson’s Ratio | 0.16~0.18
Thermal expansion coefficient | 4.0x10-6 /K
Thermal conductivity, in-plane | 20 W/K-m
Thermal conductivity, through thickness | 20 W/K-m
Minimum operating Temp (based on degradation of k under irradiation) | 600 ᵒC
Maximum operating Temp (based on void swelling) | 1000 ᵒC
Maximum allowable combined stresses | 190 MPa
*Summary, SiC/SiC Town Meeting , ORNL, January 18-19, 2000.
http://aries.ucsd.edu/Lib/PROPS/sic.html
Stress limits for using in FEM analysis:
Conventional stress limits (3 Sm) can not be directly applied to ceramics.
The SiC/SiC stress limits should take into account for the non-linear elastic behavior associated with matrix micro-cracking and matrix-fiber debonding.
Based on the summary of the ARIES Town Meeting, it was recommended to limit the total combined stress to ~190 MPa. It might be too conservative.
*A.R. Raffray et al., Fusion Engineering and Design 80 (2006)
Properties were Used in ARIES-AT*
Notes: The table shows the properties were used in the ARIES-AT thermo-mechanical analysis.

## Slide 6: ARIES-AT LiPb-Cooled SiC-Composite Divertor Could Accommodate a HF up to 5 MW/m2
Thickness of SiC front plate=0.5 mm
Thickness of W armor=3.5 mm
Cross-section of cooling channel=25x20 mm
Operating pressure=1.8 MPa
Peak heat flux=5 MW/m2
Average heat flux=1.75 MW/m2
Inlet /outlet temperature=654/764 ᵒC
Max. W temperature=~1150 ᵒC
Max. SiC temperature=~950 ᵒC
Pressure drop=~0.7 MPa
Thermal stress at SiC=~162 MPa
Primary stress at SiC=~25 MPa
Combined stresses= 189 MPa
T-shaped flow separator
Distribution of thermal stress
=45 MPa at W
*A.R. Raffray et al., Fusion Engineering and Design 80 (2006)
=162 MPa at SiC
=189 MPa at SiC
Distribution of combined stresses

## Slide 7: Update on Operating Temperature Window for SiC Composites Since ARIES-AT*
*Yutai Katoh and Lance Snead, Fusion Science and Technology, 56 (2009).
Operating temperature of he-cooled SiC-composites mainly limited by:
  High temperature swelling <2%,
  Irradiation or thermal creep strain <1% at a uniaxial stress of 100 MPa,
  Thermal conductivity through-thickness > 10 W/m-K
Yutai Katoh and Lance Snead recommended:
  Lower operating temperature > 700 ᵒC (ARIES-AT, ~600 ᵒC)
  Upper operating temperature <~1200 ᵒC
  (ARIES-AT, 1000 ᵒC)
-Preliminary design windows for 3D balanced orthogonal CVI SiC/SiC for thermal structural application
-Dotted lines indicate lack of confidence and/or experimental substantiation.
There is no update on the stress limit in literatures. The same allowable stress (190 MPa) as the ARIES-I and ARIES-AT will be assumed in FEM analysis.

## Slide 8: A SiC-Composite Finger Is Designed to Accommodate A HF up to ~5 MW/m2
Joints techniques: *H. Kishimoto, A. Kohyama, J. of Nuclear Materials
**B. Riccardi et al, Int. J. Materials and Product Technology
W/SiC composite joints using hot-pressing technique*
Holding temperature of 1500 to 1800 ᵒC
Joint shear strength as high as ~90 MPa
SiC/SiC composite joints using brazing technique**
Si-16Ti (melting temperature ~1330 ᵒC)
Si-18Cr (melting temperature ~1305 ᵒC)
or using silicone resin to joint them together at 1200 ᵒC.
Fabrication
Methods:
Step 2
Step 1
Step 3
Step 4
SiC-composite tube
Step 5
Width of Armor=26 mm
Diameter of thimble=20 mm
Thickness of thimble=1 mm
Height of the plate=70 mm

## Slide 9: Pumping Power and Stress Limits Are not Satisfied for a HF of 5 MW/m2
Operating temperature for SiC/SiC: 700 < TSiC < 1200 ᵒC
Loads and cooling conditions
  q”=5 MW/m2 (uniform), qv’’’=17.5 MW/m3
  P=10 MPa, Tin/Texit=600/700 ᵒC (450/550 ᵒC for Tallow= 1000 ᵒC)
CFX and FEM results(Not Optimized)
  Vjet=~390 m/s, HTC(Local)=9.78x104 W/m2-K
  Pp=~15% Premoved (Pp~12.5% for Tallow= 1000 ᵒC)
  Max. Tsic=1199 ᵒC(< Tallow= 1200 ᵒC) (TSiC=999 ᵒC for Tallow= 1000 ᵒC)
  Max. σp+th=~462 MPa (> σallow=~190 MPa) (σp+th=~475 MPa for Tallow= 1000 ᵒC)
Pumping power and stress limits are not satisfied.
Temperature
Velocity
Stress
Temperature-dependent properties of the W are used in the analysis
Thermal conductivity of the SiC/SiC is dependent on both irradiation temperature and fluence. In analysis, the K(T) is shown in the figure.*
*Yutai Katoh and Lance Snead, Fusion Sci. and Tech., 56 (2009).
Stress

## Slide 10: Original ARIES-Finger Configuration Is Applied in the SiC/SiC Divertor
SiC-Composite Finger
Using the original ARIES finger configuration
  VM-W thimble, cylindrical ring and W channel replaced by SiC/SiC
  ODS steel cartridge replaced by SiC/SiC cartridge
  1 mm thick SiC-composite thimble
  1 mm thick SiC-composite cylindrical ring
  2 mm thick SiC-composite front plate
  5 mm W armor
W armor and SiC composite jointed together by hot-pressing method
SiC-composite thimble, cylindrical ring and front plate jointed together by brazing method

## Slide 11: Temperature and Pumping Power Limits Are Satisfied
Operating temperature for SiC/SiC: 700 < TSiC < 1200 ᵒC
Loads and cooling conditions
  q”=5 MW/m2(uniform), qv’’’=17.5 MW/m3
  P=10 MPa, Tin/Texit=600/700 ᵒC (450/550 ᵒC for Tallow=1000 ᵒC)
CFX and FEM results
  Vjet=~191 m/s, HTC(Local)=6.52x104 W/m2-K
  Ppumping=~6.5% of the Premoved thermal (<10%) (Pp~5.7% for Tallow=1000 ᵒC)
  Max. Tsic=1120 ᵒC(< Tallow=~1200 ᵒC) (TSiC=980 ᵒC for Tallow= 1000 ᵒC)
  Max. σp+th=~212 MPa (> σallow=~190 MPa) (σp+th=~223 MPa for Tallow= 1000 ᵒC)
  Max. shear stress at the W/SiC interface σshear =~58 MPa
  The SiC thimble (1 mm thick) could be thinned to ~0.5-08 mm to meet the stress limit. However, there are too many brazing joints required.
Velocity
Temperature
Stress

## Slide 12: SiC/SiC Tube Target-Plate Cooled by Jet-Impinging Scheme Is Proposed
10 mm diameter tube ( ~4 times larger than ARIES-I tube)
½ mm thick tube
1 mm SVD-SiC layer
SiC/SiC cartridge or ODS-steel cartridge
Impinging-jet cooling scheme
Cross-section of SiC/SiC tube with impinging cooling scheme
Pol.
Rad.
Tor.
Notes: W coating and CVD-SiC layer would play a structural role after bonded together.

## Slide 13: CFX Results Indicate The Temperature and Pumping Power Limits Are Satisfied
ARIES-AT like heat-flux profile with a max. value of ~5 MW/m2 and an average of ~ 1.75 MW/m2 is assumed in the analysis
qv= ~17.5 MW/m3
Tinlet/Toutlet= 600/700 ᵒC based on SiC-composite operating temperature of 700 <TSiC< 1200 ᵒC
CFX results (some optimizations):
  Vjet=~91 m/s, Tmax. SiC=~1180 ᵒC, Tmin. SiC=~710 ᵒC, Tmax. W= 1272 ᵒC
  HCTlocal=~2.623x104 W/m2-K
  Ppumping/Premoved thermal=~3.5%
There is a large room for the pumping power to push to a higher heat flux. The cartridge can be tapered along the poloidal direction to reduce the jet velocity and rise temperature at lower heat flux region.
Velocity distribution
Temperature distribution

## Slide 14: Stress Limit Is also Satisfied Although It is very Conservative
Max. combined primary and secondary in SiC-composite tube is ~140 MPa (< σallow =~190 MPa).
Max. Combined primary and secondary stress in CVD-SiC layer (not a major structure) is ~207 MPa at low heat flux region where the temperature is the lower (~710 ᵒC).
Max. shear stress at interface is ~73 MPa
Further optimization of the cartridge to rise temperature at the lower heat flux region can reduce thermal stress.
SiC composite tube
CVD-SiC layer
SiC composite tube with W coating
140 MPa
207 MPa

## Slide 15: Summary and Conclusions
Three configurations of he-cooled SiC-composite divertor concepts have been investigated, including
  a modified finger
  an original ARIES-finger
  a tubular plate with impinging-jet cooling scheme
CFX and FEM results indicate that both configuration 2 and 3 can possibly accommodate a non-uniform heat flux with a maximum value up to 5 MW/m2 while satisfying the temperature, pumping power and stress limits.
The tubular plate design (Configuration 3) has a better thermal performance, and it is easier to be fabricated, much less brazing required, and potentially have higher reliability.